Synthesis Of 3-Alkyl And 3,4-Dialkyl Thiophene And Pyrrole Monomers: Precursors To Useful Conducting Polymers

Thiophene-based and pyrrole-based conducting polymers have a multitude of useful properties.  Synthesis of the monomers used to prepare these polymers is not necessarily straightforward or general.  Preparing substituted monomeric derivatives poses other challenges, despite the fact that such monomers lead to organic-soluble or water-soluble conducting polymers, or polymers with higher conductivities or self-orienting properties.

There are several long-term benefits of this research.

(1) New classes of organic-soluble conducting polymers.

(2) New classes of water-soluble conducting polymers

(3) Improved syntheses of known monomers.

(4) Generalized and flexible syntheses of monomers with properties predicted to give useful conducting polymers.

In addition to the research opportunities, this work will also contribute to science education.  Over the last 15 years, 50% of my graduate students have been women, including my current research group.  In addition, I have trained approximately 60 undergraduates in my research lab over the last 15 years.  I have also served as mentor to five undergraduates in the summer REU program sponsored by the NSF.  The undergraduate students have included approximately 60% women, 5 African-Americans and 2 Latino students.  Many of these undergraduates have gone on to graduate school and to successful careers in chemical industry.  The work proposed here will allow further training of both undergraduate and graduate students.

C. PROJECT DESCRIPTION

C.1 Goal:

The goal of this proposal is to synthesize substituted thiophene and pyrrole derivatives that are monomers for the preparation of conducting polymers

C.2  SPECIFIC AIMS

A. Despite the increasing importance of 3-substituted and 3,4-disubstituted thiophenes and pyrroles as monomers for conducting polymers, remarkably few synthetic routes are available.  OF these, fewer still are either general or practical.  We will explore several synthetic routes to these compounds that satisfy both requirements.

B. With suitable synthetic methods in hand, we will prepare new conducting polymers with substituents tuned to specific needs.

THE GOAL OF THIS RESEARCH IS TO DEVELOP conducting polymers that have higher conductivities, better solubility in either organic solvents or water to suit the need, and improved   To develop such polymers, the SPECIFIC AIMS of this proposal are:

(1) We will develop a practical and versatile synthetic method to 3-substituted and 3,4-disubstituted thiophenes and pyrroles from a common starting material.  We will use similar methodology to prepare benzo[c]thiophenes from phthalic acid derivatives.  1,2-Diesters, via reduction to the dialdehyde and in situ reaction with phosphorus pentasulfide, Lawesson's reagent, ammonia, or primary amines, constitutes the requisite common precursors.  Useful quantities of monomers can be prepared by this approach.

(2) Develop a practical versatile method to 3-substituted and 3,4-disubstituted thiophenes based on the reaction of the known and readily available S(CH2Li)2 with 1,2-dihalides and 1,2-diketones.  The requisite dihalides are easily prepared from a variety of alkenes, and 1,2-diketones are available from

vicinal diols, whcih are prepared by pinacol coupling of aldehydes or ketones.  Such a method will be valuable for monomer-discovery and targeted monomer design.  This method may be scaled up but will initially be used for the preparation of gram-quantities of designer-monomers.

(3) Target specific substituents for thiophene and pyrrole derivatives that will generate polymers with one or more of the following properties (a) enhanced conductivity  (b) enhanced solubility in organic solvents via incorporation of more lipophilic groups  (c) enhanced water solubility by incorporation of more polar groups.

(4) Develop new, more specific but less general, synthetic protocols for targeted monomers.

C.3  SIGNIFICANCE AND BACKGROUND

π-Conjugated poly(heterocycle)s containing five-membered rings are particularly attractive for their conductive properties.  The variety of five-membered ring poly(heterocycle)s including poly(pyrroles)s, poly(thiophene)s, poly(selenophene)s, poly(thiazole)s, poly(silole)s, poly(thiophene-1,1-dioxide)s have been prepared and studied, as there are recent reports of poly(phosphole)s and poly(imidazole)s .  The heteroatoms in the ring help control the properties of the polymers as a functional of their electron-donating or electron-withdrawing capabilities, their hydrogen-bonding abilities, and their polarizability.  These properties allow poly(heterocycles to be tuned for optimization of oxidative π-type doping, reduce n-type doping, and adjustment of the HOMO-LUMO energy levels which provide electronic transitions across a broad range of the electromagnetic spectrum.1  Poly(heterocycle)s have been used in applications that include semiconductors for field-effect transistors and LEDs, conductors for electrostatic charge dissipation and EMI shielding, as redox active materials for energy storage (batteries and super-capacitors), and as electrochromic devices.   Poly(3,4-ethylenedioxythiophene, known as PEDOT, is an outstanding example of a conductive polymer with improved redox and conductivity stability properties , relative to the parent polythiophene.groenendaal-481  The dioxane unit adds electron density to the aromatic ring, reducing both the monomer and polymer oxidation potentials, and this leads to formation of highly stable

conducting states.  Blocking the 3,4-positions also forces polymerization to the 2- and 5-positions, leading to a linear polymer chain with no α–β' coupling and fewer structural defects than most poly(heterocycle)s.  These attractive properties have led to the preparation of a number of EDOT derivatives, including 3,4-(1,3-propylenedioxy)thiophene, known as ProDOT, 3,4-(1,4-butylenedioxy)thiophene, known as BuDOT, and a series of substituted monomers that yield polymer with optimized electrochromatic properties.reynolds-6873

3,4-Ethylenedioxypyrrole has been prepared, as well as several 3,4-alkyenedioxypyrroles that give polymers with potential as electrochromic and biostable materials.  These pyrrole monomers include 3,4-(1,3-ethylenedioxy)pyrrole, known as EDOP, 3,4-(1,3-propylenedioxy)pyrrole, known as ProDOP, 3,4-(1,4-butylenedioxy)pyrrole, known as BuDOP, and monomers with alkyl groups on the ethylenalkoxy bridge.reynolds-6873  A key intermediate was dimethyl-N-benzyl-3,4-dihydroxypyrrole-2,5-dicarboxylate (2), and the cited compounds could be prepared in an additional five steps with overall yields of 20-25%.  In all cases, deprotection, hydrolysis and decarboxylation were key steps.   Pyrrole 2 was prepared from ethylenedioxythiophene precursor (1) in XXXX steps.  This series of N-substituted poly(ethylenealkoxy)pyrroles, particularly ProDOP derivatives, show reversible and long-lived electrochemistry, and useful electrochromic properties.  These polymers are rather stable in the doped state, and variation of substituents on nitrogen allows the band gap, and therefore the optical properties of the polymers, to be fine-tuned.reynolds-639  Introduction of key substituents on the propylenedioxy ring led to soluble and self-doping anodically coloring polymers, with possible use as processable electrochromics in display applications.reynolds-639

Polythiophene is an important conducting polymer that was discovered in 1980, but it is insoluble, which is the cause of many problems.  Poly(3-alkylthiophenes), abbreviated as P3ATs, are a class of polymers that exhibit good solubility, processablity, environmental stability, and electroactivity.  P3ATs are used as rechargeable battery electrodes, electrochromic devices, chemical

an optical sensors, light-emitting diodes, molecular-based devices such as micro-electrochemical amplifiers, field-effect transistors, and nonlinear optical materials.  Poly(3-alkylthiophene) was first reported in 1985 and proved to be a soluble, processable, and stable polymer.  Electrochemical polymerization and oxidative polymerization with FeCl3 has also been reported.  Methods have also been reported for the preparation of regioregular P3Ats.  It noted that electrophilic bromination of PdHTs is possible [poly(3-hexylthiophene) was employed in this example] via electrophilic bromination followed by palladium-catalyzed cross coupling reactions such as the Suzuki reaction, Stille coupling, and the Heck reaction).

Poly(3-undecylthiophene (3) is a highly conjugated polymers with good regioregularity, high conductivity, and improved environmental stability, but it is difficult to process the polymer into useful large articles.  Combination of the polymer with an insulating polymer (such as a polystyrnee compsotie) leads to a processable and mechaniscally stonrg matiral.  Poly(3-hexylthiophene) has been converted to thin film field-effect trnasitors by Langmuir-Blodgett technqueis, that were stable at the air-water interacted and couled be tansferrd onto hydrophobic substates by horizontal deposition.  Regioregular, amphiplhiic polythiophenes based of 3-dodecyl-3'(3,6,9,12-tetraoxatridecanyl)-2',5-bithoiophene are known.  Two additonal polymers, 3 from 3-bromothiiophene) and 4 from 2-bromo-3-methylthiophene have been prepared.  Both polymers are organic in common solvbents such as CHCl3, THF, and DMF, and show a regioregulararity of >95%.   Polymer 4 was found to exhibit poor moleaulr ordering and low crystallinity, and transistor deices prpeard forom this matieral showed poor field effect moblityioes.  Polyemr 3, howevr, showed high crystallinity, and the field-effect moblity is reasonably high, but ower than regioregular poly(3-hexylthiophene).bao-2607  It is noted byat 3-heteroaryl-subsituted polythiphenes have been prpared, using naphthalene, pyrnee, and indolizine subsituents, and they have intersting conductivities, electroopticalproperites such as electroluminsescence.

Although several recent synstheses of 3-subsitued thiophenes are avialble, incorporaitn of the gorup at 3- is aaccopanied by infcorpaitona of gourps and the 2- and 2,5-positons.  It is noted that 3,4-diphenylthiopehne was prpared by photochemical irradiation of diethynyl sulfides, but this approach dos not appear to be gernal or suited to our purpose.

Polypyrrole derivaitves have exhibited both positive and negative solvoconductive effects.  Poly(3,4-dimethoxyprrole) films show a highly negtive solvoconductive effect, for example.  The level of doping is also imortant t solvoconduction.  N-Subsitution of pyrrole leads to matrieals that are fdefective, and poorly condcuitng, but less defective materials are obtained from oligomers oxidized at less ositive potentials.  Polymrs derived from 3,4-disubstiuted monomers seem to mproved properties and a heavily doped poly(3,4-dimethoxypyrrole) shows an impressive reversible drop in dconductivty when exosed to a vaierty of organic vapros.zotti-2996  In the same study, poly(3,4-ethylenedioxythiophene) was insenstive to those vapors, presumably due to its poor solvating ablibty.  A combination of redox-ty0pe conduction and solvation in  poly(3,4-dimethoxypyrrole) gives it unsual solvoconductive properties, and has been used to devleop an organic solvent vapor snesor partiucarly repsonsive to chrlooform and acetonitrile.zotti-2996  A recent study showed tht conductivity is a fucntion of the solvent, and that heavily doped polymers are not sensitive to vapros, whreras lightly doped polymers do respond.

Poly(3,4-difluoropyrrole), prepared from 3,4-difloropyrrole, forms a stble polymer, in contrast to other halopyrroles which decompose (dibromopyrroles are parlticuarly unstable).  This polymer exhbits a high redox potentail, high doping levels (about 55%), and a high condocviity rlative to other poly(halopyrroles).audebert-2025  The long lifetimes of catin radical of this polymer, and the highly electrophlilic and acidic nature of the electrogenrated cation radical make it very senstive to side reacitons.audebert-2025

3-Substitued thiophenes can be prepared by several literature methods.  A recent method reacted 3-bromothiophene with alkylmagnesium halides, in the presence of a Ni(dppp)Cl2 calatyst, giving 1 in good yield (78% in THF and 61% in ether.  3-Bromorthiophene also reacts with trialkylboranes such as trihexylbornae, to give 3-hexylthiophene.  3-Bromothiphene ccan be converted to the correspsonding orgnaolmetallic (—MgBr or —Li) and condensesatin wiht aldhdyes or keotnes gives the expected alcohol via acyl addition.  This raises intersting questions of course.  How is 3-bromothiuophene prpeared and is it commerically avaialble?   3-Bromrothiophene is indeed commerically avialbe, but cost about $160/100 g.  It is expensive because direct bromination of thiphene gives 2-bromothiophne, with some 2,5-dibromothiophene.  2,5-Dibromothiophene is actually a useful synthon for preparing 3-substuted derivaitves.  After conversti to the C3 analog, the 2,5-dibromothiophene can be polymerizied directly.   In additoin, 2,5-dibromothiophene is commecially available, and not overly expensive ($72/100 g).  The brmine untis are chemicaly reacitve to many reagents, however, and this is not a genral route to 3-substituted thiuphenes if a wide range of groups and fucntionality are desired.

3-Lithiothiphenes are known, wcih can react with electorphiels, but they are formed from 2- or 2,5-disubstutied thiphenes via directed lithation.  One problme with 3-lihtiopthiophenes is their thermal instalbity, which leads to ring opening.

3-Bromothiophene is prepared by first blocking the 2- and 5-positions with removalable gourps.  If the 2- and 5-positons are blocked, bmriantoin occurs at C3.  Other halognes have been used, as well as metals such as —HgX units.  The most common approach is to prepare the diester of thiophene 2,5-

dicarboxylic acid, bromiaote, saponifiy and thermally decarboxylate.  In short, although the alkyation of 3-bromothiophene is quite attractive, it is expensive and its preparaiton is not genreal or conveneient.

Other subsitued thiophenes are known.  Compunds 3-7 have been prepared by the reactin of 3-bromothioiphenes (X2 with RLi and then suflur, followeid by multi-step tansformations.  3,4-Ethylenedisulfanylthiophene (6) and the crown ether 7 are paritucarly intrsitng monmers prepared by this method.

3-Subsituted pyrroles are attractive targets.  Once again, 3-bromopyrrole is a potnetial synthon.  Direct bormoanto of pyrrole gives 2-bromopyrrole.  However, substituents on the nitorgen atom have a profound effect on the regioseleclitivty.  1-t-Butylpyrrole, ofr example, undergoes Vismeir formayltin primairly at C3, and 1-benzenesulfonylpyrrole undergoes Friedel-Crafts benzoylaiton at C3 in the

presencence of AlCl3.   Similary, reaction of silylpyrrole 2 and NBS gives the 3-bromo derivative 3, and subsequent reactioin with butyllithium followed by an electrophiles gives 4.  The silyl gorup is easily removed by tratment with fluouiride ion, making the synthesis of 3-alkylpyrroles relatively straightforward.  An alternative prepartion reduces 3-acylpyrrorles with NaBH4 to give the 3-alkyl derivative.  Lithium aluminum hydirde can also be used for this reduction.  3-Alkylpyrroles have been prpared directly by carbonylatoin of terminal alkynes with CO and lithio-methyltrimethylsilannyl amines.

It is clear that there less need for a direct and general sysnthesi sof 3-substiuted pyrroles, alhtough 3,4-disubsitued derivitves pose synthetic problems.  One usful approach to this class of ocmpounds wa rproted by Wong, in which3,4-bis(trimethylsilyl)-1H-pyrrole (5) was converted to 6 by the gernalized scheme shown.  This is a usful, albiet lengthy route and 5 is avialbe via synthesis but not commerically avialble.  3-Aryl- and 3,4-diaryl-1H-pyrroles have also beenprpeard frm alkenes, using TOSMIC (tosylmethyl isocyanide), bnut the mehtod seems to be effeicent only when electron poor aryl gourps are present on the alkene.  A general method that produces both thiophene and pyrrole derivitves is of value, and for targeted heterocycles is essential.

thiophene monomers

biological activity?????

pyrrole monomers

new porphyrin type derivatives with interesting biology????????

C4. WORK ACCOMPLISHED

C.5. PROPOSED RESEARCH

The chemistry of thiophene and pyrrole is old, and well established.  In principle, electrophilic aromatic substitution or nucleophilic aromatic substitution reaction will produce a vast array of substituted products.  Correct!  However, the products in both cases are the 2-substituted and 2,5-substituted derivatives.  The only way to obtain 3- and 3,4-disubstituted products is to block the 2- and 5-positions of the thiophene or pyrrole ring.  Such blocking is often accomplished by first incorporating halogen, organometallic units, or carboalkoxy units into the heterocycle.  Indeed, many of the thiophene monomers are prepared by generating thiophene-2,5-dicarboxylic acid derivatives, beginning with thioglycolic acid.  To obtain the targeted compounds, a bis-decarboxylation step is required.  Such as step is straightforward, but limits the type of functionality that can be incorporated, and often leads to unwanted byproducts that can be difficult to separate.  Ethylenedioxythiophene (EDOT), for example, is sold commercially as Baytron M (W.M. Stark, $200/100 g) but contains quinoline (added to facilitate the decarboxylation), which must be removed by fractional distillation (Vigreux column) for many applications.

A direct synthetic method is called for, that does not require decarboxylation, and is compatible with a wider range of substituents.

C.5.a. 1,2-Diester Protocol.

Perhaps the most common 1,2-diesters that are readily available are esters of succinic acid (1), maleic acid (2) and fumaric acid (3).  Phthalic acid (4) is also well known, commercially available and inexpensive (ca. $49/1 Kg), as are the dimethyl and diethyl esters ($16/1 Kg and $18/1 Kg, respectively).  The acids 1-3 are commercially available and inexpensive($48/1 Kg for 1, $28/1 Kg for 2, and $15/1 Kg for 3), as are the dimethyl and diethyl esters of 1-3, although the esters are generally more expensive than the parent acid.  The esters are dimethyl succinate (DBE-4 dibasic ester, $61/500 g), dimethyl maleate ($33/1 Kg), dimethyl fumarate($113/500 g), diethyl succinate($36/1 Kg), diethyl maleate($33/1 Kg), and diethyl fumarate($76/500 g).  All diesters are easily prepared from the acid and an appropriate alcohol, of course.

In addition, alkylation and condensation reactions of succinate enolate anions are well known and very flexible with regard to incorporating functional groups as well as simple alkyl groups.  Conjugate addition reactions of diesters of both 2 and 3 are well known, again producing a variety of mono-substituted succinate derivatives.  Of great interest is the facile Diels-Alder reactivity of 2 and 3 with a variety of dienes, producing substituted and functionalized cyclohexene dicarboxylic acid derivatives.  [3+2]-Cycloaddition reactions with 2 and 3 will produce diester derivatives with interesting and variety heteroatom functionality.  Clearly, phthalic acid and it dieters can be functionalized on the benzene ring via electrophilic aromatic substitution reactions.  There is no question that esters of 1-4 can be prepared easily and with a vast assortment of substituents.

Can such derivatives be converted to thiophenes and pyrroles?  Diethyl succinate was converted to thiophene in low yield (about 30%) by heating (neat) with phosphorus pentasulfide.  In addition to thiophene, 2-alkoxythiophenes and dihydrothiophene-2-one were produced.  Alternatively, heating the disodium salt of succinic acid with phosphorus pentasulfide gave thiophene, but again in very poor yield.  In both cases, there were many products, most of which were intractable.  These results were not encouraging, and probably account for the lack of interest in this general route.  More recently, reagents have been developed that selectively convert esters to aldehydes, under the proper conditions.  Both diisobutylaluminum hydride (Dibal) and lithium tri-tert-butoxyaluminum hydride accomplish this transformation.  XXXXX has also shown that diethyl succinate reacts with Dibal (in

toluene at –78°C) to give the dialdehyde, which was reacted in situ with amines to form a bis-imine.  1,2-Diketones such as  2,3-butanedione react with Lawesson’s reagent to give 2,5-dialkylthiophenes, directly.  Surprisingly, we found no reports in the literature that reduced diesters to dialdehydes, and trapped that product with sulfur agents or ammonia to give thiophenes or pyrroles.  In our preliminary studies, we found that this sequence is quite effective.

We prepared ?????????????

Therefore, diesters are reasonable precursors to thiophenes via (a) reduction to the dialdehyde followed by (b) reaction with Lawesson’s reagent.  Similar reaction with phosphorus pentasulfide also gives the thiophene.  Based on known syntheses of diester derivatives, 3-substituted thiophenes (14), 3,4-disubstituted thiophenes (15), and thiophenes fused to cyclohexene units (16) are readily available.  In addition, diethyl phthalate is the direct precursor to benzo[c]thiophene, 17.

Another interesting route to thiophenes fused to saturated rings is based on the report that α,ω-diesters such as 17, upon treatment with LDA and CuBr give the cycloalkane-1,2-diester, 18.  This sequence provides a more versatile route to systems such as 19, where both the size of the ring and the substituent pattern can be modified.  α,ω-Diacids are easily prepared by oxidative cleavage of cyclic alkenes with ozone (oxidative workup), followed by esterification.  Therefore, virtually any cyclic alkene becomes a synthetic precursor to thiophene derivatives such as 19.

Modification of the procedures described above allows the facile synthesis of pyrroles.  All that is required is the change of Lawesson’s reagent to ammonia, or a primary amine to trap the dialdehyde.  Diesters are, therefore, synthetic equivalents for both thiophenes and pyrroles.  Pyrroles such as 20-23 are readily accessible, and Rx is modified to be H (from ammonia) alkyl (from primary alkyl amines) or aryl (from aniline derivatives).  This list includes formation of benzo[c]pyrrole (40), from diethylphthalate.

C.5.b. Dilithiomethyl Sulfide Protocol for Substituted Thiophenes.

1,2-Dihalides and 1,2-disulfonate esters, readily obtained from alkenes, would be interesting thiophene precursors, if a hydrothiophene synthon were available for direct cyclization.  One possible synthon is 30, derived from dimethyl sulfide, or a surrogate.  This dianion does not exist as drawn, but the dilithio derivative 31 is known, and has been reported to be remarkably stable in various reactions.  Sulfide 31 is prepared by treatment of 32 with butyllithium, and 32 is prepared from

Bu3SnCH2I and sodium sulfide.  The Bu3SnCH2I is prepared from ICH2ZnI (prepared from diiodomethane) and tributyltin chloride.

Preparation of 31 and treatment with 1,2-dihalides leads to the tetrahydrothiophene.   XXXX showed that simply heating tetrahydrothiophenes such as XX or XX gives the thiophene.  We therefore envision the conversion of alkenes to the dibromide and subsequent treatment with 31 will give XX or XX.  Heating, probably in situ without isolation of XX or XX, will generate the thiophene derivative.

Preparation from 1,2-diketones.

1,2-Diketones can be prepared in several ways.  Pinacol coupling of aldehydes and ketones, followed by oxidation gives the diketone.  Heating acid chlorides with pyrophoric lead gives a Wurtz-type coupling reaction that gives the 1,2-diketone.  Samarium iodide has been used in a few cases to give the same transformation.   Unsymmetrical diketones are prepared by the reaction of an acid chloride with an acyltin reagent (RCOSnBu3), in the presence of a palladium catalyst.  Another method for the preparation of 1,2-diketones treats ketones with selenium dioxide.  Both α-

ketoaldehydes and α-diketones can be prepared in this manner.  Other reagents have been reported to give similar results, but there are structural restrictions on most of them.  Diaryl diketones have been prepared by the condensation of aromatic carboxylic acids with excess lithium metal in dry THF.

The reaction of 1,4-diketones with Lawesson's reagent is well known, and the product is the thiophene.  If dilithio sulfide 31 is used with 1,2-diketones, however, the product is the 3,4-disubstituted thiophene.  Cyclization to the diketone forms the five-membered ring, and generates the dianion XX.  Subsequent treatment with aqueous acid in the workup stage leads to dehydration and aromatization to the thiophene.  This reaction sequence constitutes a new thiophene synthesis. Similar reaction with a a-ketoaldehyde leads to the 3-substituted thiophene.  Given the variety of methods for producing the diketone or ketoaldehyde, this two-step, one-pot reaction sequence is a versatile route to substituted thiophenes.

C.5.c. Targeted Polymers.

Significance

(a) Handbook of Conducting Polymers, 2nd Ed., Skothein, T.A.; Elsenbaumer, R.L.; Reynolds, J.R (Eds); Dekker, NY, 1997; (b) McCullough, R.D. Handbook of Oligo and Polythiophene; FIscher, D. (Ed.); Wiley0VCH, Weinheim, Germany, 1999; (c) Yamamoto, T. Bull. Chem. Soc. Jpn., 1999, 72, 621.

Morisaki, Y.; Aiki, Y.; Chujo, Y. "Synthesis and Properties of First Well-Defined Phosphole-Containing π-Conjugated Polymers," Macromolcuels, 2003, 36, 2594-2597.

Yamamoto, T.; Uemura, T.; Tanimoto, A.; Sasaki, S. "Synthesis and Chemical Porperties of π-Conjugated Poly(imidazole-2,5-diyl)s," Macromolecules, 2003, 36, 1047-1053.

For example, see Kaminovz, Y.; Smela, E.; Johansson, T.; Brehmere, L.; Andersson, M.R.; Ingänas, O. Synth. Met., 2000, 113, 103.

Thomspon, B.C.; Schottland, P.; Zong, K.; Reynolds, J.R. Chem. Materi., 2000, 12, 1563.

Groenendaal, L.B.; Jonas, F.; Freitag, D.; Pielarzik, H.; Reynolds, J.R. Adv. Mater., 2000, 12, 481.

Zong, K.; Reynolds, J.R. "3m,4-Alkylenedioxypyrroles: FDucntinalied Derivatives as MOnomers for New Electron-Rich COnducting and Electroactive Polymers," J. Org. Chem., 2001, 66, 6873-6882.

Kumar, A.; Welsh, D.M.; Morvant, M.C.; Piroux, F.; Abboud, K.A.; Reynolds, J.R. Chem. Mater., 1998, 10, 896.

Merz, A.; Schropp, R.; Dötterl, E. Synthesis, 1995, 795.

(a) Thomas, C.A.; Zong, K.; Schottland, P.; Reynolds, J.R. Adv. Mater., 2000, 12, 222; (b) Gaupp, C.L.; Zong, K.; Schottland, P.; Thompson, B.C.; Thomas, C.A.; Reynolds, J.R. Macromolceuls, 2000, 33, 1132; (c) Schottland, P.; Zong, K.; Gaupp, C.L.; Thompson, B.C.; Thomas, C.A.; Giurgiu, I.; Hickman, R.; Abboud, K.A.; Reynolds, J.R. Marcomolecules, 2000, 33, 7051.

ref for prep of 1 from 2.   8  or   9a b or c????

Sönmez, G.; Schwendeman, I.; Schottland, P.; Zong, K.; Reynolds, J.R. "N-Substitued Poly(3,4-propylenedioxopyrrole)s; High Gap and Low Redox Potential Swqitching electroactive and Electrochromic Polymers," Macromolcuels, 2002, 36, 639-647.

(a) Yamamoto, T.; Sanechika, K.; Yamamoto, A. J. Polym. Sci., Polym. Lett. Ed., 1980, 18, 9-12; (b) Lin, M.W-P.; Dudek, L.P. J. Polym. Sci., Polym. Lett. Ed., 1980, 18, 2869-2873.

(a) Patil, A.O.; Heeger, A.J.; Wudl, F. Chem. Rev., 1988, 88, 183-200; (b) Roncali, J. Chem. Rev., 1992, 92, 711-738; (c)Kanatzidis, M.G. Chem. Eng. News, 1990 (Dec. 3), 36-54; (d) Brédas, J.L.; Street, G.B. Acc. Chem. Res., 1985, 18, 309-315.

Scrosati, B. Applications of Electroactive Polymers, Chapman & Hall, London, 1994.

For an example, see Greenham, N.C.; Moratt, S.C.; Bradley, D.D.C.; Friend, R.H.; Holmes, A.B. Nature, 1993, 365, 628-630.

McCoy, C.H.; Wrighton, M.S. Chem. Mater., 1993, 5, 914-916.

Garnier, F.; Yassar, A.; Hajlaoui, R.; Horowitz, G.; Deloffre, F.; Servet, B.; Ries, S.; Alnot, P. J. Am. Chem. Soc., 1993, 115, 8716-8721.

For an example, see Chittibabu, K.G.; Li, L.; Kamath, M.; Kumar, J.; Tripathy, S.K. Chem. Mater., 1994, 6, 475-480.

(a) Elsenbaumer, R.L.; Jen, K.-Y.; Oboodi, R. Synth. Met., 1986, 15, 169-174; (b) Jen, K.-Y.; Miller, G.G.; Elsenbaumer, R.L. J. Chem. Soc., Chem. Commun., 1986, 1346-1347.

Sato, M.; Tanaka, S.; Kaeriyama, K. J. Chem. Soc., Chem. Commun., 1986, 873-874.

(a) Yoshino, K.; Nakajima, S.; Onoda, M.; Sugimoto, R. Synth. Met., 1989, 28, C349-C357; (b) Österholm, J.E.; Laakso, J.; Nyholm, P.; Isotalo, H.; Stubb, H.; Inganäs, O.; Salaneck, W.R. Synth. Met., 1989, 28, C435-C444.

Chen, A.-A.; Wu, X.; Riecke, R.D. "Regiocontrolled Synthesis of Poly(3-alkylthiophenes) Mediated by Rieke Zinc: Their Characterization and SOlid-State Properties", J. Am. Chem. Soc., 1995, 117, 233-244.

Li, Y.; Vamvounis, G.; Yu, J.; Holdcroft, S. "A Novel and Versatile Methodlogy for Fucnatianlization of Conjugated Polymers.  Transforamtino of Poly(3-bromo-4-hexylthiophene) via Palladium-Catlyzed Coupling Chemistry," Macromolecules, 2001, 34, 3130-3132.

See Kowaliak, J.; Tolbert, L.; Narayan, S.; Desai, P.; Abhiraman, A.S. Macromolcuels, 2001, 34, 5471-5479.

Abbett, K.F.; Teja, A.S.; Kowalik, J.; Tolbert, L. "Polymerization of 3-Undecylbithiophene and Preparation of Poly(3-undecylbithiophene)/Polystyrene COmposites in Supercritical Carbon Dioxide," Macromolcuels, 2003, 36, 3105-3019.

Xu, G.; Bao, Z.; Groves, J.T. "Langmuir–Blodgett Films of Regioregular Poly(3-hexylthiophene) as Field-Effect Transitors," LAngmuir, 2000, 16, 1834-1841.

de Boer, B.; van Hutten, P.F.; Ouali, L.; Grayer, V.; Hadziioannou, G., "Amphiphilic, Regioregular Polythiophenes," Macromolecules, 2002, 35, 6883-6892.

Bao, Z.; Lovinger, A.J., "Soluble Regioregular Polythipphene Derivatives as Semiconducting Materials for Field-Effect Trnasitiors," Chem. Mater., 1999, 11, 2607-2612.

Walsh, C.J.; Sooksimuang, T.; Mandal, B.K. "Heteroaryl Substituted Polythiophenes: Chemical and Electrochemical Syntheses and Characterizatin of Poly[3-(9-tris(ethylenea glycol) monomethyl ether) carbazoylthiophene]," MAcromolcuelses, 1999, 32, 2397-2399.

(a) 2,3-Disubstiuted pyrroles from dilithio-trialkylsilylamines.  See Jacobson, M.A.; Williard, P.G. "Synthesis of 2,3-Disubstiuted Pyrroles from 3,N-Dilithio-N-(tert-butyldimethylsilyl)-2-buten-1-amine," J. Org. Chem.,2002, 67, 32-37; (b) Palladium-catlyzed cyclisomerizxatino of en-yne-1-thoils.  See Gabriele, B.; Salerno, G.; Fazio, A. "Novel Synthesis of Subsituted Thiophenes by Palladium-Catalyzed Cycloisomerizatin of (Z)-2-En-4-yne-1-thiols,"  Org. Lett., 2000, 2, 351-352.

Lewis, K.D.; Wenzler, D.L.; Matzger, A.J., "Photochemistry of Diethynyl Sulfides: A Cycloaromatization for the Formatin of Five-Membered Rings," Organic Lett., 2003, 5, 2195-2197.

Zotti, G.; Zecchin, S.; Schiavon, G.; Groenendaal, . Chem. Mater., 2000, 12, 2996.

Roncali, J. in Handbook of COnducting Polymers, 2nd Ed., , Skotheim, T.A.; Elsenbaumer, R.L.; Reynolds, J.R. Eds, M. Dekker, New York, 1998, Chaper 12, p 312.

Vercelli, B.; Zecchin, S.; Comisso, N.; Zotti, G.; Berlin, A.; Dalcanale, E.; Groenendaal, L. "Solvoconductivity of Polyconjugated Polymers: The Roles of Polymer Oxidation Degree and Solvent Electrical Permittivity," Chem. Mater., 2002, 14, 4768-4774.

Woller, E.K.; Smirnov, V.V.; DiMagno, S. J. Org. Chem., 1998, 63, 5706.

Audebert, P.; Miomandre, F.; Di Magno, S.G.; Smirnov, V.V.; Hapiot, P. "Polymerization of 3,4-Difluoropyrrole: Electrochemical and Physicochemical Behavior of Poly(Difluoropyrrole)," Chem. Mater., 2000, 12, 2025-2030.

Audebert, P.; Bidan, G. SYnth. Met., 1986, 15, 9.

Lere-Porte, J.-P.; Moreau, J.J.E. Eur. J. Org. Chem., 2001, 1249-1258.

McCullough, R.D.; Lowe, R.D.; Jayaraman, M.; Anderson, D.L. J. Org. Chenm., 1993, 58, 904-912.  Also see Meng, H.; Huang, W. J. Org. Chem., 2000, 65, 3894-3901.

Akimoto, I.; Sano, M.; Suzuki, A. Bull. Chem. Soc. Jpn., 1981, 54, 1587-1588.

For examples see Hall, S.S.; Farahat, S.E. J. Heterocyclic Chem., 1987, 24, 1205-1213.

direct poymerization of 2,5-dibromothiphenes.

See (a) Wakefield, B.J. Organolithium Mthods, Academic Press, London, 1988; (b) Snieckus, V.  Chem. Rev., 1990, 90, 879.

Gilchirst, T.L. Adv. Heterocyclic Chem., 1987, 41, 41.

Blanchard, P.; Jousselme, B.; Frère, P.; Roncali, J. "3- and 3,4-Bis(2-cyanoethylsulfanyl)thiophenes as Building Blocks for Functionalied Thiophene-Based p-Conjugated Systems," J. Org. Chem., 2002, 67, 3961-3964.

Gilchrist, T.L Heterocylic Chemistry, 2nd Ed., Longman, Essex, UK, 1992, p 197.

Bray, B.L.; Matthies, P.H.; Naef, R.; Solas, D.R.; Tidwell, T.T.; Artis, D.R.; Muchowski, J.M. J. Org. Chem, 1990, 55, 6317.

Greenhouse, R.; Ramierez, C.; Muchowski, J.M. J. Org. Chem., 1985, 50, 2961-2965.

Masuda, H.; Tanaka, S.; Kaeriyama, K. J. Chem. Soc., Chem. Commun., 1989, 725-726.

Buchwald, S.L.; Wannamaker, M.W.; Watson, B.T. J. Am. Chem. Soc., 1989, 111, 776-777.

Liu, J.-H.; Chan, H.-W.; Wong, H.N.C. "Highly Regioselective Synthesis of 3,4-Disubstitued 1H-Pyrrole," J. Org. Chem., 2000, 65, 3274-3283.

Bray, B.L.; Mathies, P.H.; Naef, R.; Solas, D.R.; Tidwell, T.T.; Artis, D.R.; Muchowski, J.M. J. Org. Chem., 1990, 55, 6317-6328.

Smith, N.D.; Huang, D.; COsford, N.D.P. "One-Step Synthesis of 3-Aryl- and 3,4-Diaryl-(1H)-Pyrroles Using Tosylmethyl Isocyanide (TOSMIC)," Org. Lett., 2002, 4, 3537-3539.

thipphenes from thiogluyycolic acid.

Succinic ester + P2S5

succinc acid dianaion + p2s5

Larock – ester to aldhyde

Lawessons reagaent

diester to cycloalkane diester

Lich2Sch2Li prep - angew

prep 32

prep of ICH2ZnI

prep of Bu3SnCh2I

Mészáros, L. Tetrahedron Lett., 1967, 4951.

Souppe, J.; Namy, J.; Kagan, H.B. Tetrahedron Lett., 1984, 25, 2869. See also Collin, J.; Namy, J.; Dallemer, F.; Kagan, H.B. J. Org. Chem., 1991, 56, 3118.

Verlhac, J.; Chanson, E.; Jousseaume, B.; Quintard, J. Tetrahedron Lett., 1985, 26, 6075. For another procedure, see Olah, G.A.; Wu, A. J. Org. Chem., 1991, 56, 902.

For reviews of oxidation by SeO2, see Krief, A.; Hevesi, L. Ref. 10, pp. 115-180; Krongauz, E.S. Russ. Chem. Rev., 1977, 46, 59-75; Rabjohn, N. Org. React., 1976, 24, 261-415; Trachtenberg, E.N. in Augustine; Trecker, Ref. 11, pp. 119-187.

March, 5th, p 1531.

Karaman, R.; Fry, J.L. Tetrahedron Lett., 1989, 30, 6267.